| Coupling strategy for RGD peptides | Protein adsorption mass [ng/cm2] |  |  |
| --- | --- | --- | --- |
|  | 24 h | 48h | 48h after PBS-NaCl |
| NHS/EDC | 24.8 | 26.5 | 5.9 |
| Sulfo-NHS/EDC | 21.2 | 46.6 | 33.6 |